Solution-processed zinc-tin-based ternary oxide electron transport layers for planar perovskite solar cells

Saad Nadeem, Nadia Shahzad*, Sana Mehmood, Muhammad Salik Qureshi, Abdul Sattar, Rabia Liaquat, Sehar Shakir, Muhammad Imran Shahzad, and Diego Pugliese

S. Nadeem, N. Shahzad, S. Mehmood, R. Liaquat, S. Shakir

U.S.-Pakistan Centre for Advanced Studies in Energy (USPCAS-E), National University of Sciences & Technology (NUST), H-12 Sector, 44000 Islamabad, Pakistan

E-mail: nadia@uspcase.nust.edu.pk

M. S. Qureshi
Electrical Engineering and Computer Science (EECS) Department, Khalifa University, 127788 Abu Dhabi, UAE

A. Sattar
Energy Materiaux Telecommunications Research Center, Institut National de la Recherche Scientifique (INRS-EMT), G1K 9A9 Quebec, Canada

M. I. Shahzad
Nanosciences and Technology Department (NS&TD), National Centre for Physics (NCP), 44000 Islamabad, Pakistan

D. Pugliese
National Institute of Metrological Research (INRiM), 10135 Torino, Italy

Keywords: ternary metal oxide, electron transport layer, bilayer, ambient fabrication, perovskite solar cell

Perovskite solar cells (PSCs) have acquired popularity owing to their high efficiency, ease of fabrication, and affordability. In this context, the development of electron transport layers (ETLs) for highly efficient planar photovoltaic devices has received considerable attention. This study investigates the potential of zinc-tin-based ternary metal oxide ETLs for application in planar PSCs. Solution-processed methods are used to fabricate crystalline zinc stannate (Zn2SnO4), amorphous zinc-tin oxide (ZTO), and Zn2SnO4/ZTO-based bilayer films, and their structural, morphological, and optoelectronic properties are thoroughly studied. X-ray diffraction (XRD) analysis and scanning electron microscopy (SEM) images show enhanced crystallite size and better surface morphology of perovskite films deposited on bilayer ETL. Photoluminescence (PL) studies and Hall effect measurements reveal superior charge extraction, improved charge carrier mobility (21.84 cm2/Vs) and enhanced n-type conductivity in the bilayer ETL. Moreover, contact angle analysis of perovskite layer deposited on bilayer ETL shows increased resistance to moisture erosion (52.20°) which is particularly significant given the detrimental effects moisture can have on the performance of PSCs.

1. Introduction

First introduced in 2009, organic-inorganic hybrid metal halide PSCs have garnered significant interest among the solar energy community as a potential alternative to conventional photovoltaic technologies, such as silicon solar cells. Perovskite materials possess a remarkable array of characteristics, including high absorption rates, lower exciton binding energies, high charge carrier diffusion length, tunable band gaps and solution-processable low-cost fabrication methods.[1–5] Over the years, the power conversion efficiency (PCE) of PSCs has undergone substantial advancements, surging from an initial 3.8% to an impressive certified PCE of 26.1% in 2024.[6]

The primary composition of PSCs includes the following three layers: the ETL, an absorber layer and the hole transport layer (HTL). These cells can be arranged into two primary architectures, which are referred to as n-i-p (regular) planar and p-i-n (inverted) planar.[7] PSCs can be further classified, within the context of the conventional n-i-p architecture, into mesoporous and non-mesoporous, or "planar" structures.[8] While much of the past research has focused on mesoporous structures, planar configurations have gained significant interest due to their synthesis at lower temperatures and less complicated device structures, which are advantageous for industrial applications.[9] Within a conventional n-i-p architecture, the n-type compound functions as ETL, adeptly extracting and transferring photogenerated electron charge carriers from the absorber layer to the conductive fluorine-doped tin oxide (FTO) substrate. In contrast, the HTL selectively transports photogenerated holes to the rear electrode, commonly made of gold or silver. Within planar configurations, the compact ETL is crucial for collecting photogenerated electron charge carriers from the absorber layer while simultaneously functioning as a barrier for holes to impede recombination. This minimizes photovoltage losses and optimizes device performance. As a result, considerable efforts have been invested in the development of ETLs for highly efficient planar photovoltaic devices. Metal oxides with wide band gaps have gained significant interest due to their inherent qualities, including excellent optoelectronic properties, high conductivity, large dielectric constants, and superior chemical and thermal stability.[10,11] For PSC applications, wide band gap metal oxides should provide appropriate energy band alignment and high charge carrier mobility to enable optimal device performance. While TiO2 remains the widely used ETL in the production of high performance PSCs, its limitations, such as low electron mobility, higher trap states at the TiO2/perovskite junction and inadequate band-offset, have driven research towards alternative ETL materials.[12] Despite its favorable band alignment with perovskites, the use of SnO2 as an ETL can be limited by its lower conductivity and presence of surface defects leading to charge recombination.[13] Similarly, the chemical instability of ZnO ETL with the perovskite layer can adversely impact the performance of PSCs.[14]

Compared to the prevalent binary oxides, ternary oxides provide an increased level of flexibility, making it possible to fine-tune various aspects of ternary metal oxide materials through simple adjustments in their chemical composition.[15] Ternary metal oxides have recently attracted a lot of attention as effective ETLs. For instance, Ye et al. incorporated NaTaO3 ternary metal oxide ETL in PSCs and reported an efficiency of 21.07% with improved device stability.[16] Li and his team explored the potential of titanium-iron-based ternary metal oxides as alternative ETLs, discovering a decrease in surface recombination and favorable charge collection characteristics; interestingly, the perovskite device utilizing Ti0.5Fe0.5Ox attained the maximum PCE of 14.7%.[17] Similarly, Wei’s group reported the PCE of 19.8% when ZnTiO3 ternary metal oxide ETL was incorporated in PSCs.[18] Among a range of ternary metal oxides, zinc-tin-based ETLs demonstrate significant potential in PSC applications. Zinc-tin-based ternary oxides exhibit a broader band gap, high electron mobility, and a low refractive index with high chemical stability. For example, Oh et al. reported an improved electron diffusion and superior charge collection with Zn2SnO4 ETL in PSCs as compared to the conventional TiO2 with similar device performance.[19] Thambidurai et al. studied the viability of various ZTOs as potential ETL alternative in PSCs, discovering that the device with Zn1Sn1Ox/SnO2 as a bilayer ETL achieved the maximum PCE of 19.01% exhibiting enhanced charge collection and decreased charge recombination.[20] Furthermore, Shalan et al. showed that ZTO ETLs yielded better photovoltaic properties, attaining a peak PCE of 17.81%, in contrast with ZnO binary metal oxide ETLs with PCE of 12.02%.[21]

Bilayers comprising both crystalline and amorphous forms of ternary metal oxides represent a relatively untapped area of research in the development of ETLs for PSCs, offering a myriad of possibilities for further study. In addition, the research on ternary metal oxide ETLs in conjunction with mixed-cation mixed-halide perovskite absorber layer remains notably limited. In this research, a solution-based technique is employed to produce dense and uniform thin films of crystalline zinc stannate (ZS) and amorphous ZTO along with their bilayer composition. The optoelectronic properties of these materials were studied, along with their morphological analysis and compatibility with mixed-cation mixed-halide perovskite layer (Cs0.1MA0.9Pb(I0.9Br0.1)3). Essentially, the study highlights the potential of zinc-tin-based ternary metal oxides as a superior ETL alternative due to their exceptional intrinsic properties. Furthermore, improvement in optoelectronic parameters such as charge carrier mobility, surface morphology, and reduced carrier recombination were demonstrated using the ZTO/ZS bilayer ETL.

2. Results and Discussion

XRD analysis was carried out to determine the crystal structure of the deposited films. Figure 1a shows the XRD patterns of ZTO, ZS and bilayer films grown on FTO glass substrate. As previously reported, ZTO, being amorphous in nature, did not show any distinctive crystalline phase (Figure S1, Supplementary Information).[20,22] ZTO coated on FTO primarily exhibited a pattern similar to that of FTO due to its amorphous thin film.[23] The diffraction peaks observed in the ZS XRD pattern at 2 positions of 17.72, 29.14, 34.29, 35.91, 45.64, 63.51 and 68.49 correspond to hkl planes (111), (220), (311), (222), (331), (531) and (620), respectively. These characteristic peaks exhibited the highly crystalline cubic spinal phase structure of ZS (JCPDS No. 24-1470).[24] In this XRD pattern, there are no distinctive peaks of SnO2 and ZnO, neither are there any additional diffraction peaks and impurity phases which shows the successful formation of ZS film with no impurities. XRD spectrum of bilayer ETL showed a similar structure with slightly less crystallinity.

Figure 1b provides the XRD spectra for the highly crystalline Cs0.1MA0.9Pb(I0.9Br0.1)3 perovskite absorber layer deposited onto the various underlying ETLs. Prominent peaks at 14.24, 28.60 and 32.01 can be associated with the (110), (220) and (310) planes of Cs0.1MA0.9Pb(I0.9Br0.1)3, respectively, meanwhile less intense peaks correspond to (112), (211), (202), (312), (224), (314) and (404) planes, signifying the development of perovskite phase with excellent crystallinity.[25] The absence of the (001) plane for PbI2 at 12.56 indicates that the PbI2 had totally dissolved and transformed into the perovskite.[26]

The mean crystallite size (D) values related to the more intense peaks at (110) and (220) were determined for perovskite layer deposited on FTO as well as on ternary metal oxide ETLs employing the widely recognized Debye-Scherrer’s equation:[27]

| D=0.9cos | (1) |
| --- | --- |

where  denotes the X-rays wavelength,  signifies the full-width at half maximum (FWHM) in radians and  corresponds to the Bragg’s angle. The dislocation density (), which can be characterized as the measure of length of dislocation lines within a given volume unit, was also determined for both (110) and (220) peaks using the crystallite size (D) by means of the following equation:[28]

| δ=1D2 | (2) |
| --- | --- |

The D and  values of all the films, together with other crystallographic parameters, are summarized in Table 1.

Figure 1c indicates a systematic increase in the crystallite size of perovskite films when deposited on ternary metal oxide ETLs, with the greatest increase occurring with bilayer ternary metal oxide ETL. It has been discovered that the dislocation density values for perovskite films formed on ternary metal oxide ETLs decreased considerably as presented in Figure 1d. This larger crystallite size with fewer voids and dislocation densities can improve charge carrier transport resulting in overall better performance of the PSCs.[29]

Figure 1. XRD spectra of (a) bare FTO, ZTO ETL, ZS ETL and bilayer ETL and of (b) perovskite layer coated on FTO, ZTO ETL, ZS ETL and bilayer ETL. (c) Crystallite size and (d) dislocation density of perovskite layer deposited on bare FTO and ZTO, ZS and bilayer ETLs. The square and circular symbols are the experimental data, while the continuous lines are just a guide to the eyes.

Table 1. Crystallographic parameters of perovskite absorber layer deposited on bare FTO, ZTO, ZS and bilayer ETLs.

| Sample name | hkl planes | FWHM (radians) | XRD peak (2) | Intensity (a.u.) | Crystallite size (nm) | Dislocation density (10-5 lines/m2) |
| --- | --- | --- | --- | --- | --- | --- |
| Cs0.1MA0.9Pb(I0.9Br0.1)3 | (110) | 0.13 | 14.24 | 1286.05 | 62.81 | 25 |
|  | (220) | 0.16 | 28.60 | 803.85 | 53.77 | 35 |
| ZTO / Cs0.1MA0.9Pb(I0.9Br0.1)3 | (110) | 0.12 | 14.24 | 1380.86 | 67.45 | 22 |
|  | (220) | 0.15 | 28.60 | 923.68 | 56.95 | 31 |
| ZS / Cs0.1MA0.9Pb(I0.9Br0.1)3 | (110) | 0.11 | 14.24 | 1276.99 | 73.32 | 19 |
|  | (220) | 0.14 | 28.60 | 890.61 | 60.64 | 27 |
| Bilayer / Cs0.1MA0.9Pb(I0.9Br0.1)3 | (110) | 0.11 | 14.24 | 1513.39 | 77.53 | 17 |
|  | (220) | 0.14 | 28.60 | 959.12 | 60.36 | 27 |

The morphological properties of the different ternary metal oxide ETLs were studied by taking SEM images as represented in Figure 2a-c. A uniform coverage of all the ETLs was observed across the FTO glass substrate without the presence of any cracks or pinholes. Bilayer ETL, in particular, showed a rather more homogeneous and smoother coverage with comparatively larger grain size which is important for the efficient charge extraction and lower recombination at the grain boundaries.[30]

Figure 2. Top-view SEM images of (a) ZTO ETL, (b) ZS ETL and (c) bilayer ETL coated on FTO glass substrate. Top-view SEM images of Cs0.1MA0.9Pb(I0.9Br0.1)3 deposited on (d) ZTO ETL, (e) ZS ETL and (f) bilayer ETL. The most prominent very fine pinholes in panel (d) have been marked with red circles for the sake of major clarity.

The top-view SEM images of the Cs0.1MA0.9Pb(I0.9Br0.1)3 perovskite layer deposited on these ETLs show different surface morphology, as highlighted in Figure 2d-f. Perovskite film grown on ZTO ETL contains pinholes and, therefore, exhibits relatively inferior surface coverage. Whereas perovskite film deposited on ZS ETL showed better surface coverage with small grains. Notably, when comparing the perovskite films developed on ZTO and ZS ETLs, the perovskite film deposited on bilayer ETL is dense, pinhole-free, and has relatively better surface coverage with larger grain size, as demonstrated in Figure 2f. This uniform and highly crystalline perovskite structure on ETL is anticipated to boost the efficiency of PSCs.[5]

The absorbance spectra of perovskite films over FTO glass substrate and ternary metal oxide ETLs are represented in Figure 3. Perovskite film deposited on bilayer ETL exhibited the highest absorption values due to large grain size and high surface coverage ratio, as supported by the SEM results in Figure 2f. These high absorption values with bilayer ETL are crucial for superior device performance and elevated current densities.[31] In addition, the absorber layer deposited on FTO glass substrate and other ETLs has the same absorption pattern with a prominent absorption peak at ~745 nm, which is attributed to the Cs0.1MA0.9Pb(I0.9Br0.1)3 perovskite layer.[32]

Figure 3. Absorbance spectra of perovskite film coated on FTO glass substrate, ZTO, ZS and bilayer ETLs.

The investigation of the electrical properties of ETLs was conducted at room temperature through Hall effect measurements (Table S1, Supplementary Information). The negative values of bulk concentration indicate n-type nature of the charge carriers. The electron mobilities of ZTO and ZS ETLs exhibit near-identical values of 15.39 and 15.84 cm2/Vs, respectively, which is consistent with prior studies.[33] Meanwhile, the mobility of the bilayer ETL is increased to 21.84 cm2/Vs, with a slight enhancement in conductivity. The improvement in charge carrier mobility of bilayer film is attributed to its comparatively smoother coverage as discussed in SEM analysis. This relatively smooth surface reduces scattering and other obstacles that can impede the motion of the charge carriers, thus leading to more effective electron transport and extraction.[34]

The PL studies were conducted to measure the electron extraction efficiency of each layer from perovskite absorber layer. Figure 4 illustrates the steady-state PL quenching spectra of perovskite films deposited on different substrates. Interestingly, the PL intensity experienced a gradual decrease, the bilayer ETL exhibiting the lowest values. This implies that bilayer ETL is the most efficient to extract electrons from the perovskite layer as compared to the others.

Figure 4. Photoluminescence (PL) spectra of the perovskite film deposited on FTO glass substrate, ZTO, ZS and bilayer ETLs. The dotted line in correspondence of the peak is just a guide to the eyes to exclude the presence of a red shift.

Contact angle analysis was conducted in order to study the hydrophilic nature and wettability of the different layers. Figure 5 shows the water contact angle values of the analyzed ETLs and of the perovskite film deposited onto them. The bare glass substrate highlighted a fairly hydrophilic character with a contact angle of 30.90° (Figure S2a, Supplementary Information). The contact angle reduced significantly with the deposition of ETLs indicating increased hydrophilicity. Notably, the bilayer ETL exhibited the minimum contact angle of 13.00 which is beneficial for subsequent deposition of Cs0.1MA0.9Pb(I0.9Br0.1)3 perovskite film as it leads to an increase in surface energy and expedites the crystallization process for the growth of perovskite structure.[35] The lower water contact angle is also due to smooth and uniformly deposited bilayer ETL visible through SEM.

Figure 5. Water contact angle of (a) ZTO ETL, (b) ZS ETL and (c) bilayer ETL. Water contact angle of Cs0.1MA0.9Pb(I0.9Br0.1)3 perovskite film deposited on (d) ZTO ETL, (e) ZS ETL and (f) bilayer ETL.

Moreover, morphological analysis suggested that larger crystallite size in perovskite layer can result in fewer grain boundaries, which reduces the potential sites for moisture-induced degradation and improves the layer's resistance against moisture.[36] From Figure 5d-f, it can be observed that the contact angle for perovskite film grown on different ETL samples, particularly bilayer ETL, is remarkably greater than the pristine perovskite film (Figure S2b, Supplementary Information), which indicates a higher resistance to erosion by moisture and, consequently, a higher level of device stability.[37]

3. Conclusion

In conclusion, the structural, morphological and optoelectronic properties of solution-processed ternary metal oxide films as potential ETLs for PSCs were systematically investigated. XRD and SEM results showed that perovskite film crystallite size and morphology were improved when deposited on ternary metal oxide ETLs, especially for bilayer composition. These ETLs exhibited uniform coverage across the substrate, signifying efficient charge extraction. Furthermore, photoluminescence studies indicated superior charge extraction and transportation in bilayer ETL when coupled with perovskite layer. The contact angle analysis revealed increased resistance to moisture-induced degradation and improved device stability. Hall effect measurements confirmed n-type conductivity of the films, with better charge carrier mobility observed in the bilayer ETL. This study highlights the potential of zinc-tin-based ternary metal oxides as effective ETLs in high-efficiency, stable planar PSCs.

4. Experimental Section

4.1. Materials

Zinc acetate dihydrate (CAS No. 5970-45-6), zinc chloride (CAS No. 7646-85-7), tin (II) chloride dihydrate (CAS No. 10025-69-1), tin (II) chloride (CAS No. 7772-99-8), methylammonium iodide (CAS No. 14965-49-2), lead (II) iodide (CAS No. 10101-63-0), cesium bromide (CAS No. 7787-69-1), 2-methoxyethanol (CAS No. 109-86-4), N, N dimethylformamide (CAS No. 68–12-2), dimethyl sulfoxide (CAS No. 67–68-5) and fluorine-doped tin oxide (FTO) glass substrates were bought from Sigma-Aldrich (St. Louis, MO, USA). All the provided resources were utilized directly, without subjecting them to any additional purification steps.

4.2. Sample Preparation

Firstly, the FTO glass substrates were cleaned through sonication in de-ionized water, 2-propanol, acetone and 2-propanol sequentially for 15 min each. After sonication, they were dried using a nitrogen gun and plasma cleaned for 10 min. Zinc-tin oxide (ZTO) film was synthesized by reacting zinc acetate dihydrate (Zn(CH3COO)22H2O) and tin (II) chloride dihydrate (SnCl22H2O) in equimolar proportions, in 2-methoxyethanol (5 mL) solvent. Whereas acetylacetone (100 µL) was used as a stabilizing agent. The solution was kept at 60 C for 3 h under stirring. Then, it was spin coated at 3000 rpm for 30 s on an FTO glass substrate followed by annealing at 500 °C for 1 h.

The colloidal solution for the deposition of zinc stannate (ZS) thin film was prepared by dissolving 0.2 M of zinc chloride and 0.1 M of tin (II) chloride in ethanol. The precursor solution was stirred overnight at room temperature and deposited onto FTO glass substrates in the same way as ZTO film. For bilayer, a similar process was repeated for ZTO and ZS films where ZS solution was dynamically spin coated on top of the ZTO film. Following the deposition of each layer, the substrates were annealed for 1 h at a temperature of 500 C. Figure 6 provides a schematic representation of the systematic methodology involved in the preparation of ternary metal oxide electron transport layers (ETLs).

Figure 6. Methodology for the preparation of ZTO, ZS and bilayer ETLs.

The precursor solution of Cs0.1MA0.9Pb(I0.9Br0.1)3 was formulated by adding 461 mg of lead iodide, 143 mg of methylammonium iodide and 21 mg of cesium bromide in 1 mL solvent mixture composed of N, N dimethylformamide and dimethyl sulfoxide with a volumetric proportion of 4:1. The mixture was stirred at 70 C for 12 h and filtered through a 0.22 m polytetrafluoroethylene (PTFE) filter. The films were deposited onto the ETLs through a 2-step spin coating method, initially at 500 rpm for 3 s and subsequently at 4000 rpm for 30 s. A schematic representation of the perovskite layer’s deposition process is illustrated in Figure 7. During the final 10 s of the spinning process, ethyl acetate was dropped as an anti-solvent. Subsequently, the samples were annealed at 80 °C for 40 min under ambient atmosphere.

Figure 7. Schematic illustration of perovskite layer deposition.

4.3. Characterization

The structural properties and crystallite size of ternary metal oxide and perovskite films were examined using the X-ray diffraction (XRD) method, employing a Bruker D8 Advanced device (Bruker AXS GmbH, Karlsruhe, Germany) with a scan cycle of 1.25 °/min and a 2θ range between 10 and 80°. The Cu Kα radiation source (λ = 1.542 Å) was used with a 40 kV excitation voltage and a 30 mA current. Peak analysis and signal processing were performed using Jade 6.5 software from MDI (Livermore, CA, USA). The XRD spectrum of ZTO ETL deposited on FTO glass substrate is shown in Figure S1. The surface morphology of the thin films was investigated with a scanning electron microscope (SEM, JEOL Ltd., Tokyo, Japan) and images were captured at a voltage of 20.0 kV.

To determine the optical properties of ETL and perovskite films, the ultraviolet–visible–near infrared (UV–Vis–NIR) spectrophotometer UV-3600 Plus (Shimadzu Co., Kyoto, Japan) was utilized with a 2.5 µm slit width. Transmittance and absorbance measurements were taken in the 250–1100 nm range. Hall effect measurements for the evaluation of electrical properties were performed using the Ecopia HMS-3000 system (Anyang, South Korea) (see Table SI). Additionally, steady-state photoluminescence (PL) spectra were acquired with an iHR320 spectrophotometer from Horiba Scientific (Horiba Instruments Inc., Irvine, CA, USA) at an excitation wavelength of 450 nm. The surface wettability test was carried out under ambient conditions with a VCA Optima instrument (AST Products Inc., Billerica, MA, USA) utilizing a 30 µL drop of de-ionized water.

Supporting Information

Supporting Information is available from the Wiley Online Library or from the author.

Acknowledgements

D. P. acknowledges the support from the European Union - NextGenerationEU under the National Recovery and Resilience Plan (NRRP), Mission 04 Component 2 Investment 3.1 | Project Code: IR0000027 - CUP: B33C22000710006 - iENTRANCE@ENL: Infrastructure for Energy Transition and Circular Economy @EuroNanoLab.

Conflict of Interest

The authors declare no conﬂict of interest.

Data Availability Statement

The data that support the findings of this study are available from the corresponding author upon reasonable request.

References

[1]	C. Wang, D. Zhao, C. R. Grice, W. Liao, Y. Yu, A. Cimaroli, N. Shrestha, P. J. Roland, J. Chen, Z. Yu, P. Liu, N. Cheng, R. J. Ellingson, X. Zhao, Y. Yan, J. Mater. Chem. A 2016, 4, 12080.

[2]	Y. Lee, S. Lee, G. Seo, S. Paek, K. T. Cho, A. J. Huckaba, M. Calizzi, D. -W. Choi, J. -S. Park, D. Lee, H. J. Lee, A. M. Asiri, M. K. Nazeeruddin, Adv. Sci. 2018, 5, 1800130.

[3]	H. Wang, H. Yu, W. Xu, Z. Yuan, Z. Yan, C. Wang, X. Liu, M. Fahlman, J. -M. Liu, X. -K. Liu, F. Gao, J. Mater. Chem. C 2018, 6, 6996.

[4]	W. Ke, D. Zhao, C. Xiao, C. Wang, A. J. Cimaroli, C. R. Grice, M. Yang, Z. Li, C. -S. Jiang, M. Al-Jassim, K. Zhu, M. G. Kanatzidis, G. Fang, Y. Yan, J. Mater. Chem. A 2016, 4, 14276.

[5]	T. Cao, K. Chen, Q. Chen, Y. Zhou, N. Chen, Y. Li, ACS Appl. Mater. Interfaces 2019, 11, 33825.

[6]	Best Research-Cell Efficiency Chart | Photovoltaic Research | NREL, https://www.nrel.gov/pv/cell-efficiency.html, accessed: July, 2024.

[7]	I. Ermanova, N. Yaghoobi Nia, E. Lamanna, E. Di Bartolomeo, E. Kolesnikov, L. Luchnikov, A. Di Carlo, Energies 2021, 14, 1751.

[8]	W. Ke, G. Fang, J. Wan, H. Tao, Q. Liu, L. Xiong, P. Qin, J. Wang, H. Lei, G. Yang, M. Qin, X. Zhao, Y. Yan, Nat. Commun. 2015, 6, 6700.

[9]	H. Zhou, Q. Chen, G. Li, S. Luo, T. -B. Song, H. -S. Duan, Z. Hong, Y. Yang, Science 2014, 345, 542.

[10]	I. O. Oboh, U. H. Offor, N. D. Okon, Energy Rep. 2022, 8, 973.

[11]	S. Foo, M. Thambidurai, P. Senthil Kumar, R. Yuvakkumar, Y. Huang, C. Dang, Int. J. Energy Res. 2022, 46, 21441.

[12]	H. Liu, S. Hussain, D. Vikraman, J. Lee, S. H. A. Jaffery, J. Jung, H. -S. Kim, J. Kang, J. Alloys Compd. 2022, 906, 164399.

[13]	W. -J. Yin, T. Shi, Y. Yan, Appl. Phys. Lett. 2014, 104, 063903.

[14]	Z. Yang, Q. Fan, T. Shen, J. Jin, W. Deng, J. Xin, X. Huang, X. Wang, J. Li, Sol. Energy 2020, 204, 223.

[15]	J. -X. Song, X. -X. Yin, Z. -F. Li, Y. -W. Li, Rare Met. 2021, 40, 2730.

[16]	Q. -Q. Ye, M. Li, X. -B. Shi, M. -P. Zhuo, K. -L. Wang, F. Igbari, Z. -K. Wang, L. -S. Liao, ACS Appl. Mater. Interfaces 2020, 12, 21772.

[17]	X. Li, F. Hao, X. Zhao, X. Yin, Z. Yao, Y. Guo, H. Shen, H. Lin, ACS Appl. Mater. Interfaces 2017, 9, 34833.

[18]	J. Wei, F. Guo, B. Liu, X. Sun, X. Wang, Z. Yang, K. Xu, M. Lei, Y. Zhao, D. Xu, Adv. Energy Mater. 2019, 9, 1901620.

[19]	L. S. Oh, D. H. Kim, J. A. Lee, S. S. Shin, J. -W. Lee, I. J. Park, M. J. Ko, N. -G. Park, S. G. Pyo, K. S. Hong, J. Y. Kim, J. Phys. Chem. C 2014, 118, 22991.

[20]	M. Thambidurai, F. Shini, P. C. Harikesh, N. Mathews, C. Dang, J. Power Sources 2020, 448, 227362.

[21]	A. E. Shalan, A. N. El-Shazly, M. M. Rashad, N. K. Allam, Nanoscale Adv. 2019, 1, 2654.

[22]	T. Z. Oo, R. Devi Chandra, N. Yantara, R. R. Prabhakar, L. H. Wong, N. Mathews, S. G. Mhaisalkar, Org. Electron. 2012, 13, 870.

[23]	L. Kadri, A. Abderrahmane, G. Bulai, A. Carlescu, C. Doroftei, I. Motrescu, S. Gurlui, L. Leontie, M. Adnane, Nanomaterials 2023, 13, 1632.

[24]	F. Sadegh, S. Akin, M. Moghadam, V. Mirkhani, M. A. Ruiz‒Preciado, Z. Wang, M. M. Tavakoli, M. Graetzel, A. Hagfeldt, W. Tress, Nano Energy 2020, 75, 105038.

[25]	H. Choi, J. Jeong, H. -B. Kim, S. Kim, B. Walker, G. -H. Kim, J. Y. Kim, Nano Energy 2014, 7, 80.

[26]	G. Tumen-Ulzii, C. Qin, D. Klotz, M. R. Leyden, P. Wang, M. Auffray, T. Fujihara, T. Matsushima, J. -W. Lee, S. -J. Lee, Y. Yang, C. Adachi, Adv. Mater. 2020, 32, 1905035.

[27]	N. H. Touidjen, B. Bendahmane, M. L. Zeggar, F. Mansour, M. S. Aida, Sens. Bio-Sens. Res. 2016, 11, 52.

[28]	G. Turgut, E. Sönmez, Superlattices Microstruct. 2014, 69, 175.

[29]	B. Chen, Z. Yu, K. Liu, X. Zheng, Y. Liu, J. Shi, D. Spronk, P. N. Rudd, Z. Holman, J. Huang, Joule 2019, 3, 177.

[30]	S. Pang, C. Zhang, H. Zhang, H. Dong, D. Chen, W. Zhu, H. Xi, J. Chang, Z. Lin, J. Zhang, Y. Hao, Appl. Surf. Sci. 2020, 507, 145099.

[31]	Y. J. Kim, Y. J. Yoo, D. E. Yoo, D. W. Lee, M. S. Kim, H. J. Jang, Y. -C. Kim, J. -H. Jang, I. S. Kang, Y. M. Song, ACS Appl. Mater. Interfaces 2019, 11, 36020.

[32]	X. Liu, Y. Chen, Y. Miao, N. Wei, H. Chen, Z. Qin, M. Feng, Y. Wang, X. Wang, Y. Zhao, J. Phys. Chem. Lett. 2022, 13, 5088.

[33]	S. S. Shin, W. S. Yang, J. H. Noh, J. H. Suk, N. J. Jeon, J. H. Park, J. S. Kim, W. M. Seong, S. I. Seok, Nat. Commun. 2015, 6, 7410.

[34]	M. Geiger, R. Acharya, E. Reutter, T. Ferschke, U. Zschieschang, J. Weis, J. Pflaum, H. Klauk, R. T. Weitz, Adv. Mater. Interfaces 2020, 7, 1902145.

[35]	H. V. Quy, C. W. Bark, ACS Omega 2022, 7, 22256.

[36]	H. Mao, Y. Huang, Z. Ma, L. Jin, L. Tian, Y. Li, H. Yu, C. Peng, J. Mater. Sci.: Mater. Electron. 2019, 30, 3511.

[37]	R. Chen, Y. Feng, C. Zhang, M. Wang, L. Jing, C. Ma, J. Bian, Y. Shi, J. Mater. Chem. C 2020, 8, 9262.

Saad Nadeem, Nadia Shahzad*, Sana Mehmood, Muhammad Salik Qureshi, Abdul Sattar, Rabia Liaquat, Sehar Shakir, Muhammad Imran Shahzad, and Diego Pugliese

Solution-processed zinc-tin-based ternary oxide electron transport layers for planar perovskite solar cells

This study focuses on the potential of zinc-tin-based ternary metal oxides as efficient electron transport layers (ETLs) for perovskite solar cells. The research investigates the structural, morphological, and optoelectronic properties of solution-processed amorphous zinc-tin oxide, crystalline zinc stannate, and their bilayer composition, highlighting their compatibility with mixed-cation mixed-halide perovskite layer.